Section 07180 - Water Repellent / Light Consolidant for Masonry Surfaces

PART 1 - GENERAL

1.00 DESCRIPTION

This specification describes installation of water repellent/consolidant for masonry and masonry patch surfaces.

1.01 GENERAL

A. Whenever the words approved by, equivalent, or similar phrases are used in this specification, they shall be understood to mean that the material, process or item referred to shall require the written approval of the Engineer and the topping manufacturer.

B. This specification shall be read in conjunction with project specifications and/or drawings indicating the precise extent of work and the use and location of specific materials.

1.02 WORK INCLUDED

A. Provide all labor, materials, equipment and services necessary to complete the following water repellent/consolidant application work:

1. Preparation of all surfaces to receive water repellent/light consolidant. (Refer to Section 4500 Masonry Restoration with regard to cleaning and repair prior to water repellent/light consolidant treatment.)

2. Protection of surfaces not to be treated, using polyethylene sheets or removable masking agent.

3. Application of water repellent/light consolidant materials by low pressure airless spray. Application procedures and coverage rates to be employed in application of the treatment are dependent upon the condition of the substrate and the results of testing conducted at the jobsite prior to beginning general application.

1.03 RELATED WORK

A. Refer to specifications covering the following related work items:

1. Repairs and cleaning of masonry surfaces. Section 04500.

2. Repairs to expansion joints and application of joint sealants. Section 07900.

1.04 WEATHER CONDITIONS

A. The installation of, as well as the subsequent curing of all water repellent/light consolidant work shall be governed by the following:

1. No work shall commence if precipitation is expected. In case of unexpected precipitation, work shall cease immediately and all uncured work shall be covered with polyethylene tarps.

2. Normal water repellent/light consolidant application as outlined in this specification shall be carried out when ambient and subsurface temperatures during application and ultimate cure fall between 40 degrees F (4 degrees C) and 95 degrees F (35 degrees C).

3. If ambient or subsurface temperature is expected to rise above 95 degrees F (30 degrees C) during application and curing, the hot weather precautions outlined in item 3 of this section shall be followed.

4. If ambient or substrate temperatures are below 50 F (10 C), follow the cold weather precautions as outlined in Section 2, below.

5. Do not proceed with application over damp substrates. The surface should be sufficiently dry to readily observe the wetting/darkening of the spray pattern during application.

B. Cold Weather Precautions

1. Store all materials in heated area or vehicle at 65 degrees F min. (15 C) until just prior to use.

2. Do not proceed with application if temperature is below 40 F (4 C) or if ice or frost are evident on the substrate.

C. Hot Weather Precautions

1. Store all materials in cool area, 75 degrees F (24 C) max, until just before use.

2. Do not work in direct sun at temperatures above 95 degrees F (35 C).

1.05 SUPERVISION

A. Applicator must present certification from the Manufacturer that he is a Licensed Applicator for the water repellent/consolidant specified. Supervision of the execution of all work under this specification, to the extent deemed necessary by the water repellent/light consolidant manufacturer, shall be arranged and paid for by the Applicator in order to ensure that all work is carried out in strict accordance with this specification and is eligible for coverage under the Manufacturer's 5-Year Limited Warranty Program.

1.06 TESTING AND APPROVALS

A. Submit manufacturer's literature, specifications and application instructions for water repellent/light consolidant materials.

B. Testing will be conducted on each surface exposure in unobtrusive locations on representative surface conditions. Tests will employ the cleaning and other surface preparation techniques proposed for the overall project, followed by application of the specified treatment employing the proposed application procedures and equipment. General application shall not proceed until test areas are approved by the owner's representative.

1.07 Limited Warranty

A. Applicator shall be required to present a validated Certificate of Limited Warranty from the topping manufacturer, covering all defects in materials and materials performance for the five year period following installation. Applicator shall be required to execute the workmanship section of the warranty, providing five years free replacement of defective workmanship.

B. Warranty shall not include damages due to abuse, construction operations, structural settling or other latent defect in building design or construction, natural disasters such as earthquake or hurricane, or catastrophic events such as fire. Warranty shall include repair or replacement at no charge to Owner of any materials which lose effectiveness or adhesion during the five year limited warranty period.

PART 2 WATER REPELLENT/LIGHT CONSOLIDANT MATERIALS

2.00 DESCRIPTION

This specification describes the materials used in, and in conjunction with water repellent/consolidant treatment.

2.01 CLEANING MATERIALS:

- Cleaning products shall be non-ionic, detergent-based masonry building wash.  Material shall be non-corrosive, non-toxic, and water soluble.

- Products:  The following shall be assumed to meet the quality and performance requirements specified:

- “E-Wash 30”, by Edison Coatings, Inc., Plainville, CT, (860)-747-2220, or approved equal.

2.02 PERFORMANCE

A. All water repellent/consolidant materials shall be produced by a single manufacturer, and shall be eligible for coverage under the Manufacturer's 5-Year Limited Warranty program. All materials shall be delivered to jobsite in unopened containers bearing manufacturers' original labels and markings. Water repellent/light consolidant shall provide effective reduction in substrate water absorption, increase of chemical resistance to dilute acids and airborne pollutants, and shall increase the bond strength of loosened, weathered masonry surface particles to the substrate.

B. The water repellent/consolidant shall be a clear, penetrating, two component proprietary product formulated for application to vertical and horizontal masonry surfaces, and shall comply with local VOC regulations.

2.03 ACCEPTABLE PRODUCTS AND MANUFACTURERS:

A. Water repellent/light consolidant:

1. SYSTEM 90-II, as manufactured by Edison Coatings, Inc., Plainville, CT (860) 747-2220.

B. Cementitous Crack filler:

1. Pump-X 53i, as manufactured by Edison Coatings, Inc., Plainville, CT (860) 747-2220.

D. Flexible epoxy crack sealant

1. Flexi-Seal 510, as manufactured by Edison Coatings, Inc., Plainville, Ct (860) 747-2220.

2.04 STORAGE & HANDLING

A. Store all components at room temperature, off the floor, dry.

B. Observe all safety and handling information as shown on the Safety Data Sheets supplied by the Manufacturer.

PART 3: EXECUTION

3.00 DESCRIPTION

This specification describes the preparation required for various surfaces which are to receive water repellent/consolidant, and the application of same.

3.01 GENERAL

A. Prior to the application of water repellent/consolidant all surfaces must be prepared in accordance with this section of the specifications.

B. The result of this preparation shall render a surface clean, meaning having complete exposure of sound, rough surface without any deposits of contaminants, coatings, compounds, laitance, foreign, matter or loose material which could affect the bond between the surface and water repellent/consolidant materials.

C. Scaled or delaminated surfaces shall be repaired or resurfaced in accordance with specifications for masonry repair, Section 04901.

D. Surfaces to receive water repellent/consolidant must be surface dry prior to coating.

E. All caulking, patching, crack repair materials and joint sealants should be installed prior to application of the water repellent/consolidant. New patching materials shall have cured a minimum of 3 days prior to application, and shall be through-dry.

3.02 CLEANING EXISTING MASONRY AND STONE

A. General:

1. Proceed with cleaning in an orderly manner, work from top to bottom of each staging area and from one end of each elevation to the other.

2. Use only those cleaning methods indicated for each masonry material and location.

3. Perform each cleaning method indicated in a manner which results in uniform coverage of all surfaces, including corners, moldings, interstices and which produces an even effect without      streaking or damage to masonry surfaces.

4. Rinse off chemical residue and soil working upwards from bottom to top of each treated area at each stage or scaffold setting.

3.03 CRACK REPAIRS

A. All surface cracks wider than .008" (0.2mm) shall be repaired in accordance with this section of the specifications.

B. Cracks less than 1/16" (1.5 mm) wide shall be sealed after cleaning has been performed. Refer to Section 04500 and drawings for locations and methods for each type of crack and crack sealant to be used.

C. Cracks 1/16" to 1/8" wide shall be routed to a 1/2" by 1" groove, backer rod shall be installed, groove walls shall be primed with sealant primer and groove shall caulked with 2-part polyurethane sealant. Fill grooves flush with adjacent surfaces. Allow sufficient curing time for the sealant to dry-through before proceeding with water repellent/consolidant application. At least 24 hours are required.

3.04 INSTALLATION

A. Strictly observe all mix ratios. Wherever practicable, use full, pre-measured units as factory-supplied. Field mixes from drums or bulk must be consistently measured using containers calibrated in standard volume units.

B. Water repellent/consolidant shall be mixed and applied to dry surfaces by phenolic core roller or airless spray at a rate of 125-175 sq. ft. per gallon. Product shall be applied in two consecutive saturating applications ("wet-on-wet"), applied at 3 to 5 minute intervals. Minimum application temperature is 40 F.

C. Product shall be applied from the bottom of the vertical surface to the top, saturating the surface but avoiding excessive rundown. Less material will be required for the second application than for the first.

D. Protect all uncured surfaces from rain, dirt, traffic and wind-blown debris for at least 2 - 4 hours after application. For horizontal/traffic bearing surfaces, coating should be tack-free and through-cured before subjecting to traffic. Cure rate is affected by temperature and other application parameters.